**Paper No: PU-SOE-MECH-04**

**Extraction and Characterization of Vetiver Grass (Chrysopogon Zizanioides) and Kenaf Fiber (Hibiscus Cannabinus) as Reinforcement Materials for Epoxy Based Composite Structures**

[Anish Khana,b](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!) [R.Vijayc](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!) [D.Lenin, Singaraveluc](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!) [**G.R.Arpithad**](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!)[M.R.Sanjaye](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!) [Suchart Siengchine](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!) [Mohammad Jawaidf](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!) [Khalid Alamrya,b](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!) [Abdullah M.Asiria,b](https://www.sciencedirect.com/science/article/pii/S2238785419316205#!)

a. Chemistry Department, Faculty of Science, King Abdulaziz University, Jeddah, Saudi Arabia.

b. Center of Excellence for Advanced Materials Research, King Abdulaziz University, Jeddah, Saudi Arabia

c. Department of Production Engineering, National Institute of Technology, Tiruchirappalli, Tamil Nadu, India

d. Department of Mechanical Engineering, Presidency University, Bengaluru, Karnataka, India

e. Natural Composites Research Group Lab, King Mongkut's University of Technology North Bangkok, Bangsue, Bangkok, Thailand

f. Department of Biocomposite Technology, Institute of Tropical Forestry and Forest Products, Universiti Putra, Malaysia, 43400 UPM Serdang, Selangor, Malaysia

**Abstract**

The study deals with the mechanical characterization of vetiver grass fiber and kenaf fiber reinforced epoxy-based hybrid composites. Five types of [composite laminates](https://www.sciencedirect.com/topics/materials-science/composite-laminate) were developed through the hand lay-up process by varying the percentage of vetiver grass and kenaf fibers. The tensile, flexural, compression and impact tests were conducted as per ASTM. The fractured surfaces of the tested specimens were studied using a scanning electron microscope. From the results, it was shown that properties of epoxy composites were improved by hybridization with vetiver grass and kenaf fibers. The improved mechanical properties of [fiber-reinforced composites](https://www.sciencedirect.com/topics/materials-science/fiber-reinforced-composite) were noticed in increment of percentage composition of kenaf fibers.

**Keywords:**

Vetiver grass (Chrysopogon zizanioides), Kenaf fiber (Hibiscus cannabinus), Epoxy, Composites, Properties

**Publication Details:**

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Journal Name** | **Vol.** | **Month & Year**  | **Page No.** | **Publisher** | **Scimago Ranking** |
| Journal of Material Research and Technology | 9(1) | Jan. 2020  | 773-778 | Elsevier | Q2 |