**Paper No: PU-SOE-PHY- 08**

**Synthesis, Thermal Stability and Structural Transition of Cubic SnS Nanoparticles**

S.S. Hegdea, Prashantha Muraharib, **Brian Jeevan Fernandesb#,** R.Venkateshc, K. Rameshb

a. Department of Physics, CMR Institute of Technology, Bengaluru 560 037, India.

b. Department of Physics, Indian Institute of Science, Bengaluru 560 012, India.

c. Centre for Material Science, KLE Technological University, Hubballi, 580031, India

#.Department of Physics, Presidency University, Bangalore.

**Abstract**

Recently identified cubic polymorph of SnS (SnS-CUB) is a promising low-cost material for solar cell applications. We report on the thermal stability, structural and optical properties of SnS-CUB nanoparticles. The average crystallite size of cubic SnS nanoparticles synthesized by wet chemical method at 20 °C is about 34.9 nm and unit cell lattice parameter a = 11.59 Å. We found that cubic phase remained structurally stable up to 400 °C even though sulfur is partially re-evaporated. The sample annealed at 450 °C contains both cubic and orthorhombic phases. When the annealing temperature is increased to 500 °C, the sample completely transforms to orthorhombic structure. Raman spectroscopy showed the formation of minor secondary phases Sn2S3 and SnO2 at temperatures ≥500 °C. Three distinct regions of weight loss are observed in thermogravimetric curve (TGA) of cubic SnS nanoparticles; around 300 °C, 600 °C and 800 °C. Weight loss of 10% observed near 600 °C was due to rapid re-evaporation of sulfur from SnS. Annealing at 500 °C decreases the direct optical bandgap value 1.68 eV–1.3 eV (direct), 1.0 eV (indirect) is also an indication of the structural transition of SnS-CUB to orthorhombic SnS. Cubic SnS nanoparticles were strongly absorbing light photons in the visible wavelength range of 400 nm–700 nm. The orthorhombic SnS with an indirect bandgap of 1 eV has extended the absorption edge to 1000 nm. By combining both cubic and orthorhombic SnS, the absorption can be extended to a wide wavelength range.

**Keywords:**

Cubic SnS, nanoparticles, TGA, Thermal stability, Optical properties.

**Publication Details:**

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Journal Name** | **Vol.** | **Month & Year**  | **Page No.** | **Publisher** | **Scimago Ranking** |
| Journal of Alloys and compounds | 820 | April, 2020 | 153116 | Elsevier | Q1 |